## Slide 1: Investigation of Current Efficiency in Molten Oxide Electrolysis for Carbon-Free Production of Ferromanganese Master’s Thesis Author: Håkon Ulvik Supervisor: Dr. Braulio Beltran-Pitarch (NTNU) Co-Supervisors: Assoc. Prof. Espen Sandnes (NTNU) Dr. Gøril Jahrsengene (SINTEF)

## Slide 2
Background and Motivation
Steel is important
Today SAF – Tomorrow MOE
Manganese is very important for steel
MOE process for iron already developed
CO2 free process

## Slide 3
Objectives
Solve the climate crisis

## Slide 4
Theory
Electrons go brrrrr

## Slide 5
Experimental

## Slide 6
Experimental
13 different experiments
  Cathodic current densities
    1.0 A/cm2, 1.5 A/cm2, 2.0 A/cm2, 2.5 A/cm2
  MnO concentration in the melt
    1:1 MnO:CaO
    10 mole%, 20 mole%, 30 mole%, 40 mole%
  Runtimes
    1 h, 2 h, 3 h, 4 h
  Temperature
    1300oC, 1350oC, 1400oC
  Co-Reduction of MnO and FeO
  Synthetic Air atmosphere

## Slide 7
Results and Discussion

## Slide 8
Results and Discussion

## Slide 9
Limitations and Uncertainties

## Slide 10
Conclusion and Further Work

## Slide 11
Acknowledgements
This Master’s Thesis is part of the ZeSiM project - Zero Emission Silicon and Manganese production through electrowinning. The project funded by the Research Council of Norway (Grant No. 344259) and The Norwegian Ferroalloy Producers Research As-sociation (FFF) with its partner companies Eramet, Elkem, Finnfjord, and wacker, whose support is gratefully acknowledged.

## Slide 12: Variants in the template
In this template you can choose between the following templates:
Blue top with white background, white top with blue background, and green top with white background. In addition, we have some variants without the logo in the upper right corner that can complement the other templates where appropriate.
We recommend using the same variant throughout the presentation. The next slide shows how to choose the different variants.
NOTE: Delete the slides you don't need for your presentation.

## Slide 13: Use ready-made layouts
2

## Slide 14: Six content tips
Keep the text simple and minimize the amount of text
Use the notes field for keywords and additional information
Use graphics/images to convey your message
Keep a common thread in background and graphics colors
Tell stories
Creating a good presentation takes time
NB: Do not use PowerPoint's design suggestions uncritically.
More tips:
https://support.microsoft.com/en-us/office/tips-for-creating-and-delivering-an-effective-presentation-f43156b0-20d2-4c51-8345-0c337cefb88b

## Slide 15: Text sizes (universal design)
The font size should be at least 28 for content and at least 32 for headings.
In figures, graphs, boxes and similar, the text often has to be smaller.
Powerpoint has a built-in feature to check for universal design. Read more about it and universal design of presentations here:
https://i.ntnu.no/wiki/-/wiki/English/Universal+design+of+presentations+and+slides

## Slide 16: Automatic subtitling (universal design)
With PowerPoint for Microsoft 365, you can have what you say as you present transcribed, and the words appear on screen as captions in the same language you're speaking, or as subtitles translated into another language. This can help accommodate individuals in your audience who are deaf or hearing impaired, or who have more familiarity with another language.
Read more about live, automatic captioning for the hearing impaired or subtitles in PowerPoint:
https://support.microsoft.com/en-us/office/present-with-real-time-automatic-captions-or-subtitles-in-powerpoint-68d20e49-aec3-456a-939d-34a79e8ddd5f

## Slide 17: Color contrast (universal design)
The color chart in this template contains several NTNU support colors + NTNU blue.
Examples of good enough contrast for text on a colored background:
Choose one of the two darkest colors in the color chart for white (negative) text on a colored background. And preferably bold text.
Choose one of the two lightest colors in the color chart for black/dark text on a colored background.
NB: NTNU has more support colors than in this template:
https://i.ntnu.no/wiki/-/wiki/Norsk/Farger+i+grafisk+profil

## Slide 18: Reset an image
If you are going to copy images that have been cropped (such as the image on this slide) to a new presentation, but do not want to include the cropping – in this case in the arc at the top and around the NTNU logo – do the following:
Select the image > Go to the Picture Format tab, tap the button that the image shows > Select reset image.
Test on this slide.
Photo: Geir Mogen

## Slide 19: Storytelling Template – Title
This text box automatically expands in height according to the amount of text (this also applies to the title box). Be sure to move both the title box and the body text box so that they are in a place on the image without important image information. The title box must be adjusted in width according to the title length. If the title is on multiple lines, move the title box so that it is glued on top of the body text box.
This is a template made specifically for storytelling.
Keep the title and text short. Instead, use the notes field for the entire story.
Find a good image.
Click the image icon in the middle of the page to insert the image.
The text boxes on the left have animations, the image appears first, then the text boxes animate on the second tap.
The next slide shows the template with the image.
Delete this text box before use.

## Slide 20: Storytelling Template - Title
This text box automatically expands in height according to the amount of text (this also applies to the title box). Be sure to move both the title box and the body text box so that they are in a place on the image without important image information. The title box must be adjusted in width according to the title length. If the title is on multiple lines, move the title box so that it is glued on top of the body text box.
Photo: Geir Mogen

## Slide 21: Frequently used icons
Education and studies
Research
Find/search
About us/department/units
Career, continuing education
Internationalization/alumni
Library
Innovation
Vacancies (in contact box)
Employees (in contact box)
Email
Map marker/visiting address/location
Phone (in contact box)
Time
See the rest of the icon library by clicking "Insert" > "Icons" and search for what you want.

## Slide 22: Example of graphics in boxes
Right-click on the icon and select "Change graphics" > "From icons"
The following slides contain examples of NTNU design.
Lorum ipsum
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorum ipsum
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorum ipsum
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorum ipsum
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Lorem ipsum lor
Also check out NTNU's own image database: https://ntnu.fotoware.cloud/fotoweb/

## Slide 23: Example of graphics
Right-click on the icon and select "Change graphics" > "From icons"
LOREM IPSUM
Lorem ipsum lore lorem ipsum lorem
LOREM IPSUM
Lorem ipsum lore lorem ipsum lorem
LOREM IPSUM
Lorem ipsum lore lorem ipsum lorem
LOREM IPSUM
Lorem ipsum lore lorem ipsum lorem
LOREM IPSUM
Lorem ipsum lore lorem ipsum lorem
LOREM IPSUM
Lorem ipsum lore lorem ipsum lorem
LOREM IPSUM
Lorem ipsum lore lorem ipsum lorem
LOREM IPSUM
Lorem ipsum lore lorem ipsum lorem
LOREM IPSUM
Lorem ipsum lore lorem ipsum

## Slide 24: LAYOUT EXAMPLE Lorem ipsum lorem ipsum lore lorem ipsum lorem ipsum
1
2
LOREM IPSUM
Lorem ipsum lorem ipsum lore lorem ipsum lorem ipsum
3
LOREM IPSUM
Lorem ipsum lorem ipsum lore lorem ipsum lorem ipsum
4
LOREM IPSUM
Lorem ipsum lorem ipsum lore lorem ipsum lorem ipsum
5
LOREM IPSUM
Lorem ipsum lorem ipsum lore lorem ipsum lorem ipsum
Lorem ipsum dolor sit amet, consectetur adipiscing elit, sed do eiusmod tempor incididunt ut labore et dolore magna aliqua.

## Slide 25: Timeline example
1 april
Lorem ipsum lore lorem ipsum lorem ipsum
4 may
Lorem ipsum lore lorem ipsum lorem ipsum
7 april
Lorem ipsum lore lorem ipsum lorem ipsum
12 april
Lorem ipsum lore lorem ipsum lorem ipsum
19 march
Lorem ipsum lore lorem ipsum lorem ipsum
27 march
Lorem ipsum lore lorem ipsum lorem ipsum

## Slide 26: Circular timeline example
27 march: Lorem ipsum lorem lorem ipsum
19 march:
Lorem ipsum lorem lorem ipsum
12 april:
Lorem ipsum lorem lorem ipsum
25 April: Lorem ipsum lorem lorem ipsum

## Slide 27: Chart example
43%
LOREM IPSUM
79%
LOREM IPSUM
52%
LOREM IPSUM
Chart: Title
| Cat 1 | Cat 2 | Cat 4 | Cat 5 | Cat 6 | Cat 7 | Cat 8 | Cat 9 | Cat 10
Graf | 9 | 7 | 4 | 7 | 2 | 6 | 8 | 9 | 4
.
.2

## Slide 28: Layout example with graphics
LOREM
Lorem ipsum
LOREM
Lorem ipsum lorem ipsum
LOREM
Lorem ipsum
LOREM
Lorem ipsum lorem ipsum
LOREM
Lorem ipsum
LOREM
Lorem ipsum lorem ipsum
LOREM
Lorem ipsum
LOREM
Lorem ipsum lorem ipsum
LOREM
Lorem ipsum
LOREM
Lorem ipsum lorem ipsum
You can cover the entire surface with a picture or illustration.

## Slide 29: Layout example with images
LOREM
Lorem ipsum lorem ipsum
LOREM
Lorem ipsum
LOREM
Lorem ipsum lorem ipsum
LOREM
Lorem ipsum
LOREM
Lorem ipsum lorem ipsum
LOREM
Lorem ipsum
LOREM
Lorem ipsum lorem ipsum
LOREM
Lorem ipsum
LOREM
Lorem ipsum lorem ipsum
LOREM
Lorem ipsum
You can cover the entire surface with a picture or illustration.

## Slide 30: Layout example
LOREM
Lorem ipsum lorem lorem
LOREM
Lorem ipsum lorem lorem
LOREM
Lorem ipsum lorem lorem
LOREM
Lorem ipsum lorem lorem
If you replace the background image, please note that the text must be readable.
Photo: Adobe Stock

## Slide 31: Closing slide