## Slide 1: Effect of Process Variables on Current Efficiency and Metal Composition
Master’s Thesis in Electrochemical Engineering
Supervisor: Co-Supervisors: Dr. Braulio Beltran-Pitarch (NTNU) Assoc. Prof. Espen Sandnes (NTNU) & Dr. Gøril Jahrsengene (SINTEF)
Author: Håkon Ulvik
Defence date:
06.07.2026

## Slide 2: Background and Motivation
Steel is fundamental for modern society
Manganese (Mn) is the third most common alloying element in steel
Most Mn is in the form of ferromanganese (FeMn)
Submerged Arc Furnaces (SAF)
Boston Metal and MIT have developed MOE for Fe

## Slide 3: Objective
Expand our knowledge about which variables affect the current efficiency & metal composition

## Slide 4: Theoretical Framework
Basicity
  Quantifiable number that is related to melt properties
  Metallurgical: weight fractions, melt behaviour
  Optical: molar fractions, corrosivity of melt against refractory materials
Current Efficiency
  How much of the charge goes into the desired reactions
  Want this to be as close to 100% as possible
  Hall-Heroult: 95%

## Slide 5: Experimental - Setup
Gas out
Alumina radiation shields
B-type thermocouple
Tungsten (W) Quasi-Reference
Inert anode (SPS Cr90Fe10)
Consumable iron cathode
Alumina crucibles
Melt
Gas in
Fe
O2 gas bubbles
Anode
Closed vertical tube furnace
Galvanostatic electrolysis
Spark Plasma Sintering (SPS)
Characterised with SEM-EDS

## Slide 6: Conclusions from Specialisation project
Successful electrolysis using MOE and oxygen evolving electrode, producing a FeMn alloy when only MnO is present was demonstrated
Higher Mn valency leads to drastic reduction in CE
Excessive oxygen production from higher valences might reduce CE because of re-oxidation.
High reactivity of higher valences, more oxides along the crucible walls.
Melts with only MnO can be assumed to operate stably
Pre-reduction of the manganese oxide ore seems to be (as assumed) necessary before electrolysis.

## Slide 7: Experimental - Experiments
RUNTIME
1 h
2 h
3 h
4 h
CURRENT DENSITY
1.0 A cm-2
1.5 A cm-2
*2.0 A cm-2
2.5 A cm-2
TEMPERATURE
1300oC
1350oC
1400oC
CO-REDUCTION Fe Mn
1 mole% FeO
SYNTHETIC-AIR ATMOSPHERE
200 ml min-1
MnO CONCENTRATION
40 mole%
30 mole%
20 mole%
10 mole%

## Slide 8: Results and Discussion

## Slide 10: Results and Discussion – Current Density
Constant variables | 
Temperature | 1300oC
Runtime | 4 h
[MnO] | 30 %
[SiO2] | 40%
[CaO] | 14.1 %
[MgO] | 10%
[Al2O3] | 5.9%
Total Basicity | 1.105
Optical Basicity | 0.747
Viscosity [Pa s] | 0.540

## Slide 11: Results and Discussion – MnO Concentration
Constant variables | 
Temperature | 1300oC
Runtime | 4 h
icathodic | 1 A cm-2
[SiO2] | 40%
[MgO] | 10%
[Al2O3] | 5.9%
 | 10% | 20% | 30% | 40%
Optical Basicity | 0.747 | 0.747 | 0.747 | 0.747
Total Basicity | 1.007 | 1.056 | 1.105 | 1.155
Viscosity [Pa s] | 0.873 | 0.690 | 0.540 | 0.417

## Slide 12: Results and Discussion – MnO Concentration
Constant variables | 
Temperature | 1300oC
Runtime | 4 h
icathodic | 1 A cm-2
[SiO2] | 40%
[MgO] | 10%
[Al2O3] | 5.9%
 | 10% | 20% | 30% | 40%
Optical Basicity | 0.747 | 0.747 | 0.747 | 0.747
Total Basicity | 1.007 | 1.056 | 1.105 | 1.155
Viscosity [Pa s] | 0.873 | 0.690 | 0.540 | 0.417

## Slide 13: Results and Discussion – MnO Concentration
Constant variables | 
Temperature | 1300oC
Runtime | 4 h
icathodic | 1 A cm-2
[SiO2] | 40%
[MgO] | 10%
[Al2O3] | 5.9%
 | 10% | 20% | 30% | 40%
Optical Basicity | 0.747 | 0.747 | 0.747 | 0.747
Total Basicity | 1.007 | 1.056 | 1.105 | 1.155
Viscosity [Pa s] | 0.873 | 0.690 | 0.540 | 0.417

## Slide 14: Results and Discussion – Runtime
Constant variables | 
Temperature | 1300oC
icathodic | 1 A cm-2
[MnO] | 30 %
[SiO2] | 40%
[CaO] | 14.1 %
[MgO] | 10%
[Al2O3] | 5.9%

## Slide 15: Results and Discussion – Temperature
 | 1300oC | 1350oC | 1400oC
Mn [wt%] | 27.3 | 21.0 | 13.1
Fe [wt%] | 63.4 | 72.8 | 81.1
Si [wt%] | 4.0 | 3.3 | 2.7
Other [wt%] | 5.3 | 2.9 | 3.1
Current efficiency | 1300oC | 1350oC | 1400oC
Mn | 21.87% | 23.00% | 24.03%
Si | 12.53% | 14.14% | 19.37%
Other | 4.20% | 3.28% | 6.67%
 | 1300oC | 1350oC | 1400oC
Viscosity [Pa s] | 0.540 | 0.396 | 0.296

## Slide 16: Results and Discussion – Co-Reduction
Temperature | 1300oC
Runtime | 4 h
icathodic | 1 A cm-2
[MnO] | 29 %
[FeO] | 1%
[SiO2] | 40%
[CaO] | 14.1 %
[MgO] | 10%
[Al2O3] | 5.9%

## Slide 17: Results and Discussion – Co-Reduction
Temperature | 1300oC
Runtime | 4 h
icathodic | 1 A cm-2
[MnO] | 29 %
[FeO] | 1%
[SiO2] | 40%
[CaO] | 14.1 %
[MgO] | 10%
[Al2O3] | 5.9%
10 mm
10 mm
Anode
Cathode
QRE
Anode
Cathode
QRE

## Slide 18: Results and Discussion – Co-Reduction
Temperature | 1300oC
Runtime | 4 h
icathodic | 1 A cm-2
[MnO] | 29 %
[FeO] | 1%
[SiO2] | 40%
[CaO] | 14.1 %
[MgO] | 10%
[Al2O3] | 5.9%

## Slide 19: Results and Discussion – Synth.-Air Atmosphere
Temperature | 1300oC
Runtime | 4 h
icathodic | 1 A cm-2
[MnO] | 30 %
[SiO2] | 40%
[CaO] | 14.1 %
[MgO] | 10%
[Al2O3] | 5.9%

## Slide 20: Results and Discussion – Synth.-Air Atmosphere
Temperature | 1300oC
Runtime | 4 h
icathodic | 1 A cm-2
[MnO] | 30 %
[SiO2] | 40 %
[CaO] | 14.1 %
[MgO] | 10%
[Al2O3] | 5.9%

## Slide 21: Results and Discussion – Synth.-Air Atmosphere
Temperature | 1300oC
Runtime | 4 h
icathodic | 1 A cm-2
[MnO] | 30 %
[SiO2] | 40%
[CaO] | 14.1 %
[MgO] | 10%
[Al2O3] | 5.9%
8.1g of metal (excluding cathode tip)
Current Efficiency | 
Mn | 28.42%
Si | 16.19%
Other | 1.39%

## Slide 22: Conclusions
A cathodic current density of 1 A cm-2 is indicated to perform best
MnO concentrations above 30 mole% results in little improvement
The atmosphere above the melt had no significant impact on performance.
Current efficiency reduces drastically with runtime
  Dissolution, reoxidation
Increasing temperature, improved electrochemical conditions, but resulted in high amounts of impurities.

## Slide 23: Further Work

## Slide 24
This Master’s Thesis is part of the ZeSiM project - Zero Emission Silicon and Manganese production through electrowinning, a joint project between NTNU and SINTEF. The project is funded by the Research Council of Norway (Grant No. 344259) and The Norwegian Ferroalloy Producers Research As-sociation (FFF) with its partner companies Eramet, Elkem, Finnfjord, and wacker, whose support is gratefully acknowledged.